## Slide 1
Introduction to Berry Curvature effects in transport
experiments in topological matter
Luttinger Karplus theory of AHE
Berry connection as intracell coordinate
Berry curvature and real-space spin texture
Planar Hall effect
Quantized anomalous Hall effect
Supported by GB Moore Foundation, DOE, NSF
N. P. Ong, Princeton Univ.

## Slide 2
Karplus-Luttinger theory of the anomalous Hall effect (1955)

## Slide 3
All textbooks
Equations of motion should include Luttinger term with Berry curvature
Luttinger (‘54, ‘64)
Quinn Luttinger
Adams, Blount (‘59)
Karplus, Luttinger (‘54)
Implication for Hall current -- existence of a transverse current
that is field antisymmetric and dissipationless.
In most crystals, vanishes by TR invariance and inversion symmetry
Anomalous velocity

## Slide 4
Intracell coordinate in wave packet motion
Luttinger, Kohn, Roth, Blount, … Berry, Niu, …
Present in all crystals, but vanishes by symmetry if time-reversal and inversion symmetry are both present.
Wannier coord. R
with the intracell coordinate
The Berry curvature “lives in” k-space.
is absent by symmetry in Si, Ge, GaAs, Cu, Ag etc
is finite in ferromagnets (TRI broken)

## Slide 5
Adams-Blount derivation of Luttinger eqn
The intracell coordinate acts like a vector potential in k –space.
The Berry curvature is the curl of
fails to commute with itself.
Extra term in the velocity
Adams, Blount ‘59
, or

## Slide 6
Identify “connection”
Hereafter, relabel as
Buried implications of Luttinger’s theory
1. The intracell coordinate cannot be ignored.
2. Existence of Berry curvature and anomalous velocity in all crystals
3. The anomalous Hall effect in ferromagnets is a direct manifestation of

## Slide 7
Intrinsic vs extrinsic (skew scattering) mechanism for anomalous Hall effect (AHE)
Karplus Luttinger theory (intrinsic)
is independent of lifetime
Skew-scattering theory (extrinsic)
Experimental results supported both predictions
But from measurements vs. T in one sample
The anomalous Hall effect
saturates at low H
Mimics saturation of M

## Slide 8
Science 2004
In spinel CuCr2Se4, magnetization M
arises from direct exchange between S
(local moments) in Cr.
Itinerant carriers play no role in exchange.
Increasing dopant Br depletes carriers.
Allows ideal platform to investigate
how AHE is affected by altering carrier density
with M unchanged.

## Slide 9
As x(Br) is varied from 0.1 to 1, changes
by 3 decades and by ~6 decades.
AHE is intrinsic in CuCr2Se4 spinel
Strong evidence supporting
and a dissipationless Hall current.

## Slide 10
Berry phase and Berry Curvature

## Slide 11
Spin ½ in precessing magnetic field (written as R(t))
The Berry phase of an electron in a tilted field
Berry vector potential
(connection)
usual dynamic phase
geometric (Berry) phase
R(t)
Closed loop C
Michael Berry

## Slide 12
Berry potential 1-form
Eigenstates
Berry curvature 2-form
Has form of monopole field (strength ½)
1-form vs vector rep.
Berry curvature vector
is tedious to calc. but
surprisingly simple!
Nakahara

## Slide 13
Area of cap
Berry flux
Hence Berry phase equals the Berry flux piercing cap
g = 1/2
Berry phase, Berry flux and solid angle

## Slide 14
Berry curvature from real-space spin textures

## Slide 15
Phys. Rev. B 57 (1998)
Interpreted the giant anomalous Hall effect
in terms of a phase arising from
chiral canting of local moments
(solid angle) Holstein (PR, 1968)
As e hops, Hund’s rule
locks to
electron
Mn moment

## Slide 16
Science 2001
Within each tetrahedron, Mo and Nd moments
are canted.
Leads to spin textures (cones).

## Slide 17
Berry curvature from spin textures
Produces large AHE.

## Slide 18
PRL 2009
MnSi, FeGe are metals in B20 symmetry class
Large Dzyaloshinsky-Moriya exchange term
Favors spiral spin textures
Exhibit skyrmions (radial twist of spins)
Carriers scattered from skyrmion spin texture
acquire large Berry phase.

## Slide 19
If carriers move in a spin environment
with dense spin chirality
they acquire a giant AHE from
Berry curvature.
In MnSi, Lee et al. estimate the
equivalent field is 100 Tesla!
AHE vanishes if H aligns all moments.
Giant Hall conductivity from spin texturre
Emergence in MnSi of giant AHE in a narrow interval 0.1—0.4 Tesla under pressure

## Slide 20
Planar anomalous Hall effect

## Slide 21
Tian Liang et al., Nat. Phys. 2018
A semimetal with Dirac like hole pocket at .
However, Dirac node is not protected (small gap at node).
Many unusual features in MR and Hall effect in tilted H.

## Slide 22
Large AHE signal even when H lies in plane of applied current (planar Hall effect).
First known example of (true) planar Hall effect.
Planar field H produces a Berry curvature Ω that is normal to plane.
H
Planar Hall geom.
Ω

## Slide 23
Quantized Anomalous Hall Effect

## Slide 24
Pauli matrices
Band structure of graphene
By analogy with the precessing spin ½ problem,
At Dirac node, we have a monopole Berry curvature.
E(k)
kx
ky
In one valley K
0
Mimics a spin ½ in a magnetic field
Basis is Wannier 2-spinor

## Slide 25
At each k, the “field” maps to a direction on unit sphere
Qi, Wu, Zhang, PRB (2006, 2008)
Qi, Hughes, Zhang, PRB (2008)
Shoucheng Zhang
Map of 2D Brillouin Zone to unit sphere
As k roams over a patch in BZ, traces a patch on sphere.
If map of full BZ covers the sphere once, the Chern number C = 1

## Slide 26
Chern number C and xy
Thouless et al (TKNN), 1982
2-band Hamiltonian given by
maps d(k) from BZ torus to the unit 2-sphere S2.
Chern number is the no. of times wraps around S2
The 2D Hall conductivity of Chern insulator is the Chern number .
Qi, Wu, Zhang PRB (06, 08)
2D Brillouin zone (torus)
sphere
kx
ky
d

## Slide 27
The TKNN conductivity (PRL, 1982)
Berry curvature
Wannier coord in Bloch rep
Perturbed wave func. to first order in H1
Velocity along y axis
To eliminate vy matrix inside sum, use
Velocity in linear response
David Thouless
Kohmoto 1985

## Slide 28
Berry vector potential (connection)
Sum over all k
states to get
Define
Its curl is

## Slide 29
Topological Insulators (TI), Bi2Se3, Bi2Te3
Fu, Kane, PRB 2007
Qi, Hughes, Zhang, PRB 2008
States are insulating in the bulk.
Surface states have band-inversion with Dirac states at crossings.
Nodes are protected at TRIM (time-reversal invariant momenta)
by time-reversal invariance.
TRIM
kx
ky
If TRI is broken in a magnetic field H or by ferromagnetism,
all Dirac nodes are gapped, leaving metallic chiral edge states.
Edge states will exhibit AHE in zero H.
Surface BZ of TI
Charlie Kane

## Slide 30
Qikun Xue et al., Science 2013
Qikun Xue

## Slide 33
Berry phase effects on electronic properties, Xiao, Chang Niu, RMP 2010
References
Anomalous Hall effect, Nagaosa et al., RMP 2009
Topological Insulators and Topological Superconductors, Bernevig and Hughes
Princeton Press 2013
General theorem relating the bulk topological number to edge states in two-dimensional
Insulators, Qi, Wu and Zhang, PRB 74, 045125 (2006)
Quantized Hall Conductance in a Two-Dimensional Periodic Potential,
Thouless, Kohmoto, Nightingale and den Nijs, PRL 49, 405 (1982).
Geometry, Topology and Physics, M. Nakahara (Taylor Francis)
Elementary Differential Geometry, Barrett O’Neill