## Slide 1
Intro to the Thermal transport
in the Kitaev magnet -RuCl3
The planar thermal Hall conductivity Kxy. Czajka et al., Nat Mater. 2022
Berry curvature or Majoranas?
Chiral edge modes occupied by bosons
Chern number
2. Oscillations in thermal conductivity Kxx in QSL state
Univ. of Tennessee
Oak Ridge National Lab
Supported by GB Moore Foundation, DOE, NSF
Princeton Univ.
A. Banerjee
(Purdue U.)
D. Mandrus
S. Nagler
P. Lampen-Kelley
JQ Yan
Princeton, July 12, 2023
Czajka et al., Nat. Phys. 2021
Peter Czajka
Tong Gao
Max
Hirschberger
(RIKEN, Tokyo)
NPO
Nick Quirk

## Slide 2
Replace each spin by 1 bj and 3 cj Majoranas
Its excitations are Majoranas and vortices (“visons”)
(Kitaev, Annals Phys., 2006)
Jackeli and Khaliullin (PRL, 2009) realized Kitaev’s Hamiltonian in
transition metal oxides with edge shared tetrahedra.
Using Majorana representation, Kitaev obtained the exact ground-state (B=0).
The Kitaev honeycomb model
Community identified -RuCl3 as best proximate.
Exchange frustration

## Slide 3
Takagi et al., Nat. Rev. Phys. 2019
Jackeli-Khaliullin realization of the Kitaev model in Ir and Ru chalcogenides
Strong spin orbit coupling  lone hole occupies Jeff = ½ doublet
In the Ru-Ru-Cl2 plane, quantum interference btw 2 paths
Suppresses direct exchange
Results in Ising exchange with  normal to plane
Edge-sharing octahedra
Ru-Ru-Cl2 plane
Jackeli, Khaliullin, PRL 2009
spin orbit coup.

## Slide 4
Lattice structure and Kitaev spin axes in -RuCl3
Kim and Kee, PRB (2016)
Sy
Sz
Sx
Crystals are highly susceptible to stacking fault formation.
(Kitaev, Annals Phys., 2006)

## Slide 5
Phase diagram of -RuCl3 (with B || a)
-RuCl3 is closest proximate to Kitaev QSL
(Plumb, Sears, Banerjee, Lampen-Kelley,
Leahy, Hentrich, Kasahara, …)
In plane H of 7.3 T suppresses zigzag order
QSL state stable in interval (7.3, 11.6 T).
Is the thermal Hall conductivity half-quantized?
Kasahara et al. Nature (2018)
Yokoi et al. Science (2021)
terms lead to AF zigzag state
below 7 K with B=0.

## Slide 6
Nature 2018
Measurements from 3.7 to 4.9 K. What happens below 3.7 K?

## Slide 7
Measurements of thermal conductivity tensor Kij
heater
5-mil Au wire
Delrin post
zigzag
armchair
With , we measure
Infer
Thermal current density JQ
Sample 1
Sample 2
We measure the thermal resistivity matrix .
Then invert to get thermal conductivity matrix .

## Slide 8
Major challenge in Kxy expt. -- I) Magnetocaloric Effect
Effects of magneto-calorific effect and eddy-current heating

## Slide 9
Mirror symmetry, handedness, and Thermal Hall Effect
B aligned normal to mirror.
Preserves mirror symmetry.
Thermal Hall current JQ (or Kxy) must vanish!
B aligned parallel to mirror plane.
Breaks mirror symmetry.
Allows finite JQ (Kxy) to exist.
, JQ are polar
B is axial

## Slide 10
300 µK
H
No thermal Hall signal from 0.29 to 5 K for
Resolution to 50 µK, uncertainty of
B||a
B||b
With H||a, thermal Hall signal emerges above 3 K.
First reported by Kyoto group (Yokoi et al.)
Peter Czajka

## Slide 11
Curves of vs. B at fixed T
Inferred curves of vs. B
For B>10 T and T<4 K, has huge uncertainties (product of 0 and
is strongly T dependent at all B measured.
Non-intersecting curves of suggests taking fixed-T cuts.

## Slide 12
B a
Thermal Hall signal antisymm. in B
Color map of in B-T plane
Small negative region
Planar thermal Hall effect for B || a
T = 7 K
Verify
But
Confirms findings of Yokoi et al. (Science 2021)
~50 curves

## Slide 13
Berry Curvature and chiral edge modes

## Slide 14
Luttinger anomalous velocity
Berry curvature Wall potential U
Neutral excitations can exhibit a thermal Hall effect (Hirschbeger et al., Science 2015)
Leads to a chiral edge thermal current.
In a thermal gradient , a finite Kxy emerges.
x
y
warm
cool
See Nagaosa et al., Rev. Mod. Phys. 2010

## Slide 15
Thermal Hall conductivity Kxy (semiclassical)
Kane, Fisher (1996)
Cooper, Halperin (1997)
Matsumoto, Murakami (2011)
Niu (2011)
Luttinger velocity vA
Berry curvature
Chern number
wall potl
Bose-Einstein distrib. .
Bose distrib -
x
U(x)
y
J
Q
x
bath
T
A
T
B
T
C
heater
Edge current
W

## Slide 16
Matsumoto and Murakami
(2011, 2014)
Microscopic theory of
Luttinger velocity vA
Berry curvature
Chern number
Bose-Einstein distrib. .
Semiclassical derivation
Winding number
x
y
warm
cool

## Slide 17
Chern, Zhang, Kim, PRL 2021
Finite Berry curvature in spin excitation bands of Kitaev magnet
McClarty, et al., PRB (2018)
Joshi, PRB (2018)
Chern, Zhang, Kim, PRL (2021)
In -RuCl3,
reverses sign with H a
H comprised of J, K and terms
Planar Hall geometry
H

## Slide 18
Czajka, Gao, Hirschberger
Fermions or Bosons in edge mode?
2
Fermion (arb. units)
boson
2
boson
For fermions, is T independent.
Two band fit
Kane Fisher (1996)
Data verify bosons
Fermion (arb. units)

## Slide 19
Grey data represent important deviations from Murakami’s expression.

## Slide 20
Overall scale of is fixed by = 1
Chern-number check:
In universal units
B > 9 T)
Consistent with = 1

## Slide 21
Check for energy of lowest band
At 7 T, energy = 1 meV
In close agreement with dominant
sharp mode seen in
ESR
THz microwave absorption
Neutron scattering

## Slide 22
Evidence against a phonon planar Hall effect in -RuCl3
Profiles of Kxx vs T qualitatively different from Kxy vs. T

## Slide 23
Summary of planar thermal Hall results
Kxy signal appears above T ~ 3 K for B || a.
Kxy/T is very strongly T dependent.
Fits very well the edge-mode Hall effect for bosons (Murakami)
Consistent with topological magnons above 10 T with = 1, and a Berry curvature
that changes sign with B || a. (Zhang, Chern, Kim)
Spin-mode energy agrees with THz experiments.
First observation of edge-mode, bosonic Hall effect.
Definitely not fermionic edge modes; not half-quantized.
A phononic mechanism is ruled out.

## Slide 24
Oscillations in Kxx

## Slide 25
Oscillation amplitude decreases as T rises, but planar Kxy increases
Damping of amplitude consistent with Lifshitz-Kosevich form
]
Fit yields effective mass
m* = 0.67 me
Oscillations (bulk, fermionic?) and planar Kxy (edge, bosonic) seem to involve different populations of spin excitations
Osc. ampl.
Kxy
Czajka et al., Nat. Phys. 2021

## Slide 26
Oscillations in Kxx emerge below 4 K with
H || a
H || a
Amplitude largest in interval 7 – 11.5 T (QSL state)
Above 11.5 T, Kxx steps up to an H-independent value
Below 7 T, weak oscillations resolved in zig-zag phase
Czajka et al., Nat. Phys. (2021).
Czajka, Gao, Hirschberger

## Slide 27
Amplitude function is large in QSL state
Amplitude is large in QSL (7.3 < B < 11.5 T).
Abruptly vanishes above 11.5 T. Extends as a weak tail to 4 T in zigzag phase (mixed phase?).

## Slide 28
“Index plot” of integer increment Δn vs 1/H
Extrema of plotted vs 1/H
Sample 1 (blue symbols) and 3 (red) measured with .
Open triangles and circles are from 1 in tilted H (tilt angles θ = 39o and 55o).
The 5 data sets fall on straight segments (with break at ~7 T).
Oscillations mimic Landau-level oscillations, but there are no free electrons!
Gap is 2 eV (from ARPES). At 1 K, free electrons are exponenty suppressed.
Effective “Fermi surface” area = 30 T (below 7 T) and 41 T or 64 T (above 7 T).
H
θ
a
c

## Slide 29
Reproducibility of oscillation period and phasing
Plot vs. H shows that sequence is not periodic in H.
Extrema of curves of are used in index plot.
Strong reproducibility in period and phasing across 5 data sets from 3 samples.

## Slide 30
Crystal with multiple stacking faults
Multiple
Transitn model
(withdrawn)
Crystal without stacking faults
PRB 2015

## Slide 31
ORNL recent results Zhang, Yan et al. Arxiv 2303…
TN = 6.5 K
TN = 7.6 K
Czajka et al. Nat Phys

## Slide 32
Thank you
Peter Czajka
Tong Gao
Max
Hirschberger
(RIKEN, Tokyo)
NPO
A. Banerjee
(Purdue)
D. Mandrus
S. Nagler
P. Lampen-Kelley
JQ Yan